## Slide 1
Introduction and point groups
Stereographic projections
Low symmetry systems
Space groups
Reciprocal Lattice & Diffraction
Deformation and texture
Interfaces, orientation relationships
Martensitic transformations
Crystallography
H. K. D. H. Bhadeshia

## Slide 13
Construct reciprocal
lattice section normal
to [001]

## Slide 14
Cubic P, section of reciprocal lattice normal to [001]

## Slide 15
Reciprocal
lattice
section
normal
to [110]

## Slide 16
Cubic P, section of reciprocal lattice normal to [110]
001
110
_

## Slide 18
Cubic P, section of reciprocal lattice normal to [111]
110
_
_

## Slide 21
For 100 keV accelerating voltage, the wavelength of electrons is 0.0037 nm.
If the d spacing is 0.2 nm, then the Bragg angle is just 0.5°
Consider now the Bragg law in reciprocal space

## Slide 24
Cubic P
Cubic F

## Slide 25
Cubic P [011]
Cubic F
_
111

## Slide 26
Cubic P [111]
Cubic F
022
_
220
_

## Slide 28
Diffraction from thin crystals

## Slide 30
200 nm thick foil
50 nm thick foil

## Slide 31
[111]
[1 1 0.9]

## Slide 32
(R. Herring)

## Slide 36
Cubic-F
lattice parameter 3.566 Å

## Slide 39
Su et al.
2014