## Slide 1
Martensite
Bainite
Alloy design: strong bainite
Widmanstaetten ferrite
Allotriomorphic ferrite
Pearlite
Overall kinetics
TRIP steel
TWIP steel
Mitigation of residual stress
Bulk nanostructured steel
Steels
H. K. D. H. Bhadeshia
www.phase-trans.msm.cam.ac.uk/teaching.html

## Slide 2
Problem: to design a bulk nanocrystalline steel which is very strong, tough, cheap ….
(courtesy of M. Endo)

## Slide 4
an apple weighs
1 Newton
1 m
= 1 Pa

## Slide 5
Pure iron, Brenner (1956)

## Slide 6
Scifer, 5.5 GPa and ductile
Kobe Steel

## Slide 7
field ion microscope
image

## Slide 9
1 Denier: weight in grams, of 9 km of fibre
50-10 Denier
Scifer is 9 Denier

## Slide 10
Claimed strength of carbon nanotube is 130 GPa
Edwards, Acta Astronautica, 2000
Claimed modulus is 1.2 TPa
Terrones et al., Phil. Trans. Roy. Soc., 2004

## Slide 11
Strength of whiskers decreases with size
Strength of a nanotube rope 2 mm long is less than 2000 MPa

## Slide 12
Strength produced by deformation limits shape: wires, sheets...
Strength in small particles relies on perfection. Doomed as size increases.
Summary

## Slide 13
Smallest size that can be achieved in a polycrystalline substance?

## Slide 14
Yokota & Bhadeshia, 2004

## Slide 15
Thermomechanical processing limited by recalescence
Summary
Need to store the heat
Reduce rate
Transform at low temperature

## Slide 16
adapted using selected data from
Tsuji et al. Scripta Mat. 47 (2002) 893

## Slide 17
Fine crystals by transformation
Introduce work-hardening capacity
Need to store the heat
Reduce rate
Transform at low temperature

## Slide 18
Swallow and Bhadeshia, 1996

## Slide 20
1 µm
Cementite suppressed using silicon

## Slide 23
wt%
Low transformation temperature
Bainitic hardenability
Reasonable transformation time
Elimination of cementite
Austenite grain size control
Avoidance of temper embrittlement

## Slide 26
200 Å
g
g
a
a
a
Caballero, Mateo, Bhadeshia

## Slide 28
Low temperature transformation: 0.25 T/Tm
Fine microstructure: 20-40 nm thick plates
Harder than most martensites (710 HV)
Carbide-free
Designed using theory alone

## Slide 29
Hammond and Cross, 2004
Velocity km s-1
Stress / GPa

## Slide 30
Paul Davies, Tata Steel, 2012

## Slide 31
“more serious battlefield threats”

## Slide 32
ballistic mass efficiency
consider unit area of armour

## Slide 41
200 Å
g
g
a
a
a
Very strong
Huge uniform ductility
No deformation
No rapid cooling
No residual stresses
Cheap
Uniform in very large sections

## Slide 42
Zhang & Yang, 2019
wind turbines +rolling mill, vibration machinery

## Slide 43
Fang, Yang, Liu, Song, Fang, Bhadeshia, Materials and Design, 50 (2013) 38
Cannot easily be welded

## Slide 45
Chatterjee & Bhadeshia, 2004
Fe-1.75C-Si-Mn wt%
2104